## Slide 1
(a) (b) (c)

## Slide 2
(a) (b) (c)
Cumulative LEED pattern (electron energies between 2.5 and 17 eV) measured at room temperature on the clean Ge(110) surface. The diffuse background of the inelastically scattered electrons is removed for every single images in the constituting series. The Ge(110) surface exhibits a c(2x8) structure, see B.Z. Olshanetsky, S.M Repinsky, and A.A. Shlyaev, Surf. Sci. 64, 224 (1977).
MicroLEED pattern (electron energy 3 eV) measured at room temperature in the wake were at high temperatures an eutectic droplet passed by (see the SI for more images). The arrows point at the faint signals that are related to a centered 2 by 2 structure in the substrate. The diffuse background of the inelastically scattered electrons is removed.
Cumulative LEED pattern (electron energies between 1.5 and 21 eV) measured at room temperature in the wake were at high temperatures an eutectic droplet passed by (see the SI for more images). The diffuse background of the inelastically scattered electrons is removed for every single images in the constituting series. Line scans of the specular beam in out-of-phase conditions (not shown here) show a clear broadening along the [001] direction compared to the [1-10] direction, which evidence a large step density of steps running in the [1-10] direction. The five-fould periodicity along the [001] direction of the surface unit cell is in perfect agreement with a fitting of 4 armchair “units” (with length a*sqrt(3)) of a germanene ribbon along 5 Ge(110) surface unit cells in the [001] direction, leading to a zigzag-terminated nanoribbon along the steps in the [1-10] direction. In the [1-10] direction the lattice constant of the germanene ribbon fit very well with the Ge lattice constant in that direction.