## Slide 1: Charge Noise Measurements SQ22-79-5-2-1
03 February 2023

## Slide 2: About the sample
2x2d2s
S2P Leaking to GND: Not sure it is fridge problem or device problem
 Kept at 0V all the time
S1B1 has very little effect but enough to have a dot
SET Studied for charge noise

## Slide 3: Procedure
1) Measure dc scan of several Coulomb peaks
2) Take the first 12 peaks and note in a table the voltages of the valleys
3) Choose an ‘optimal currents’ for charge noise measurement on the left flanges an note it in a table
4) For each peak
a. Go in the valley and measure charge noise
b. Increase by steps of 0,05 mV the plunger gate voltage to reach the optimal current
c. Repeat step b. after few seconds to take into account drift
d. Lower the voltage by 4 mV normally in the valley but not sure
f. Repeat a,b,c,d two more times
g. Make a dc scan showing two peaks  The right one is the one that was measured
h. Measure Coulomb diamond
Automatic
Manual

## Slide 4: Technical details
DC measurement Bias : Vdc = 1,01 mV bias x 100 mV/V (Vib module)
DC measurement Current Measurement : M1g Module 100 MV/A with Keithley settings
Charge noise measurements : Keithley settings
A constant current offset has to be removed

## Slide 5: Measurement Code
station.hardware.boundaries['S1P'] = (1000,2000)
duration_minutes = 10
repeats = 3
optimal_current_a = np.array([60,100,160,300,400,450,500,550,600,650,650,600])*1e-12
valleys_a = [1682,1692,1701,1711,1721,1731,1741,1750,1760,1769,1779,1788]
calibrate_range = 0.1
step = 0.02
it_n = 2500
gate_param = station.gates.S1P
time_trace_param = KeithleyDMM6500_digitizer_parameter(station.keithleyA, duration_minutes, 'Idc', 'V', 2e3)
m_instr = [time_trace_param]
for k in range(len(valleys_a)):
gate_param(valleys_a[k])
optimal_current = optimal_current_a[k]
print(f'Valley {k+1}: \n')
for i in range(repeats):
print(f'Repeat {k+1}: \n')
#Charge Noise Valley
time.sleep(2)
ds=do0D(*m_instr,name=f'Charge Noise Valley (repeat {i+1}), Gain 100M A/V').run()
#Sweep from Valley to Slope
stop = False
iteration = 0
av = 0
while abs(av - optimal_current)>2e-12:
I=[]
for o in range(10):
I.append(station.I_dcA())
av = np.average(I)
if av > optimal_current:
gate_param(gate_param()-step)
elif av < optimal_current:
gate_param(gate_param()+step)
hf.printProgressBar(iteration, it_n)
if iteration > it_n:
break
iteration +=1
#Charge Noise Slope
stop = False
iteration = 0
av = 0
time.sleep(5)
while abs(av - optimal_current)>2e-12:
I=[]
time.sleep(2)
for o in range(30):
I.append(station.I_dcA())
av = np.average(I)
if av > optimal_current:
gate_param(gate_param()-step)
elif av < optimal_current:
gate_param(gate_param()+step)
hf.printProgressBar(iteration, it_n)
if iteration > it_n:
break
iteration +=1
ds=do0D(*m_instr,name=f'Charge Noise Slope (repeat {i+1} of peak {k+1}), Gain 100M A/V').run()
do1D(gate_param, gate_param(), gate_param()-5, 20, 0.01,
station.I_dcA, reset_param=False, name=f'manual tuning to Valley {gate_param} (repeat {i+1} of peak {k+1})').run()
ds = do1D(gate_param, gate_param()-10, gate_param()+10, 500, 0.01,
station.I_dcA, reset_param=True, name=f'DC scan peak {k+1}'.format(gate_param)).run()
Fast_param=station.gates.Vsd_1m
Fast_start=-40
Fast_end=40
Fast_npoint=121
Fast_delay=0.01
Slow_param=station.gates.S1P
Slow_start=station.gates.S1P()-10
Slow_end=station.gates.S1P()+10
Slow_npoint=81
Slow_delay=0.01
do2D(Fast_param,Fast_start,Fast_end,Fast_npoint,Fast_delay,Slow_param,Slow_start,Slow_end,Slow_npoint,Slow_delay,station.I_dcA,name=f'Coulomb Diamond peak {k+1}',reset_param=True).run()

## Slide 6: Full Scan
uuid: 1675360149109255110
optimal_current_a = np.array([60,100,160,300,400,450,500,550,600,650,650,600])*1e-12
valleys_a = [1682,1692,1701,1711,1721,1731,1741,1750,1760,1769,1779,1788]
Points chosen
1
3
2
4
5
6
7
8
9
10
11
12

## Slide 7: Peak 1 , Current targeted = 60 pA, Voltage valley = 1682 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675361426493255110 | 15 | OK | 1675362090368255110 | 50 | Drift at beginning
2 | 1675362702847255110 | 15 | OK | 1675363386167255110 | 55 | OK
3 | 1675363998738255110 | 15 | OK | 1675364687812255110 | 60 | Jump at end
1675365298260255110
1675365320550255110

## Slide 8: Lever arm

## Slide 9
Alpha = 0.92 +- 0.01
Charge noise = 0.696
Alpha = 0.71 +- 0.02
Charge noise = 0.459

## Slide 10: Peak 2 , Current targeted = 100 pA, Voltage valley = 1692 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675365796554255110 | 10 | OK | 1675366467956255110 | 80 | Drift down
2 | 1675367080442255110 | 10 | OK | 1675367768323255110 | 100 | Drift down
3 | 1675368380952255110 | 10 | OK | 1675369084329255110 | 80 | Drift down
1675369694773255110
1675369717362255110

## Slide 12
Orange
Alpha = 1.34 +- 0.01
Charge noise = 0.887
Red
Alpha = 1.25 +- 0.01
Charge noise = 0.487

## Slide 13: Peak 3 , Current targeted = 160 pA, Voltage valley = 1701 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675370195862255110 | 15 | OK | 1675370894263255110 | 120 | Drift down
2 | 1675371506902255110 | 15 | OK | 1675372198705255110 | 150 | ok
3 | 1675372811505255110 | 10 | OK | 1675373562102255110 | 130 | Drift down
1675374172802255110
1675374195146255110

## Slide 15
Orange
Alpha = 0.94 +- 0.01
Charge noise = 1.402
Red
Alpha = 1.32 +- 0.01
Charge noise = 0.765

## Slide 16: Peak 4 , Current targeted = 300 pA, Voltage valley = 1711 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675374665329255110 | 10 | OK | 1675375432172255110 | 270 | Drift down
2 | 1675376755117255110 | 10 | OK | 1675376755117255110 | 270 | Drift down
3 | 1675377367951255110 | 10 | OK | 1675378078141255110 | 300 | Drift down
1675378688896255110
1675378711123255110

## Slide 18
orange:
Alpha = 0.94 +- 0.01
Charge noise = 0.999
red:
Alpha = 0.86 +- 0.02
Charge noise = 0.646

## Slide 19: Peak 5 , Current targeted = 400 pA, Voltage valley = 1721 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675379175620255110 | 15 | OK | 1675379871178255110 | 380 | Drift down
2 | 1675380483962255110 | 10 | OK | 1675381186103255110 | 340 | Drift down
3 | 1675381798904255110 | 15 | OK | 1675382505771255110 | 400/600 | jump
1675383116499255110
1675383138872255110

## Slide 21
Alpha = 1.42 +- 0.01
Charge noise = 1.313

## Slide 22: Peak 6 , Current targeted = 450 pA, Voltage valley = 1731 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675383600443255110 | 15 | OK | 1675384288260255110 | 400 | Drift down
2 | 1675384901111255110 | 15 | OK | 1675385624022255110 | 380 | Drift down
3 | 1675386236777255110 | 15 | OK | 1675386928347255110 | 380 | jump
1675387539174255110
1675387561679255110

## Slide 24
Alpha = 1.45 +- 0.01
Charge noise = 0.693

## Slide 25: Peak 7 , Current targeted = 500 pA, Voltage valley = 1741 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675388021764255110 | 15 | OK | 1675388841793255110 | 480 | Drift down
2 | 1675389454551255110 | 15 | OK | 1675390214482255110 | 480 | ok
3 | 1675390827261255110 | 15 | OK | 1675391563250255110 | 480 | Drift down
1675392173980255110
1675392196251255110

## Slide 27
Alpha = 1.20 +- 0.02
Charge noise = 0.487

## Slide 28: Peak 8 , Current targeted = 550 pA, Voltage valley = 1750 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675392655797255110 | 20 | OK | 1675393513099255110 | 500 | Drift down
2 | 1675394125940255110 | 15 | OK | 1675394922686255110 | 520 | Drift down
3 | 1675395535513255110 | 15 | OK | 1675396225197255110 | 500 | Drift down
1675396835978255110
1675396858947255110

## Slide 30
Alpha = 0.79 +- 0.01
Charge noise = 0.980

## Slide 31: Peak 9 , Current targeted = 600 pA, Voltage valley = 1760 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675397320047255110 | 20 | OK | 1675398028609255110 | 500 | Drift down
2 | 1675398641431255110 | 15 | OK | 1675399394208255110 | 550 | Drift down
3 | 1675400007000255110 | 20 | OK | 1675400720811255110 | 600 | Drift down
1675401331663255110
1675401354598255110

## Slide 33
Alpha = 1.08 +- 0.01
Charge noise = 0.607

## Slide 34: Peak 10 , Current targeted = 650 pA, Voltage valley = 1769 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 1675401814932255110 | 150 | Drift Up | 1675402598105255110 | 500 | Drift down
2 | 1675403211029255110 | 30 | OK | 1675404018132255110 | 550 | Drift down
3 | 1675404630997255110 | 30 | OK | 1675405470505255110 | 650 | Drift down
1675406081290255110
1675406104186255110

## Slide 36
Alpha = 0.75 +- 0.02
Charge noise = 1.104

## Slide 37: Summary for the first 10 CoulombPeaks
peak | Vp | Lever arm (eV/V) | slope (A/V) | charge noise (ueV/sqrt(Hz)) | uuid | 
1 | 1686 | 0.348757487 | 2.95E-07 | 0.696 | 1675363386167255110, | TLS
2 | 1697 | 0.323528773 | 4.21E-07 | 0.887 | 1675367768323255110, | 
3 | 1707 | 0.316750456 | 4.87E-07 | 1.402 | 1675372198705255110, | 
4 | 1717 | 0.276639482 | 8.21E-07 | 0.999 | 1675376755117255110, | TLS
5 | 1727 | 0.27783133 | 9.90E-07 | 1.313 | 1675381186103255110, | 
6 | 1737 | 0.233213263 | 1.19E-06 | 0.693 | 1675385624022255110, | TLS
7 | 1747 | 0.241645396 | 1.55E-06 | 0.487 | 1675390214482255110, | TLS
8 | 1757 | 0.215836589 | 1.58E-06 | 0.98 | 1675394922686255110, | 
9 | 1768 | 0.222497763 | 1.98E-06 | 0.607 | 1675399394208255110, | 
10 | 1778 | 0.22158971 | 2.07E-06 | 1.104 | 1675404018132250000, | TLS

## Slide 38: Points
Fit to the log (CN paper) result in lower charge noise
Charge noise in MultiLayer devices is comparable
Lever arm = 0.2?
Fit the single spectra to
No screening?

## Slide 39: Things to have
TEM 7nm QW with plane counting
Raman 2D map (check after Ge substrate I can try to do it at VLL)
HBs measurements -> percolation and mobility
Fit of the Mobility density to the Monroe (reference?)
Tau_q was about 4ps lower then SQ21_81_5

## Slide 40
The measurements in the next 4 slides were taken at the top of the respective peaks, this was done manually.
I still have to check them (Davide)

## Slide 41: Peak 5: top time trace 1728 mV
1675434129190255110

## Slide 42: Peak 6: top time trace 1738 mV
1675436388918255110
Notes: {'measurement_type': '1D_sweep', 'gate_name': 'S1P', 'V_swing': 10.0, 'npt': 200, 't_meas': 50.0, 'biasT_corr': False, 'average': 40, 'diff': False, 'sample_rate': 100000000.0, 'acquisition_delay_ns': 500, 'n_columns': 4, 'line_margin': 1, 'bias_T_RC': 100, 'enabled_markers': [], 'differentiate': False, 'dataset_id': 1779, 'dataset_uuid': 1675441166652255110, 'sample_info': "<class 'core_tools.data.SQL.connect.sample_info'>"}

## Slide 43: Peak 7: top time trace 1748 mV
1675443265684255110
JUMP
Notes: {'measurement_type': '1D_sweep', 'gate_name': 'S1P', 'V_swing': 10.0, 'npt': 200, 't_meas': 50.0, 'biasT_corr': False, 'average': 40, 'diff': False, 'sample_rate': 100000000.0, 'acquisition_delay_ns': 500, 'n_columns': 4, 'line_margin': 1, 'bias_T_RC': 100, 'enabled_markers': [], 'differentiate': False, 'dataset_id': 1781, 'dataset_uuid': 1675442424495255110, 'sample_info': "<class 'core_tools.data.SQL.connect.sample_info'>"}

## Slide 44: Peak 8: top time trace 1758 mV
1675445603245255110
Notes: {'measurement_type': '1D_sweep', 'gate_name': 'S1P', 'V_swing': 10.0, 'npt': 200, 't_meas': 50.0, 'biasT_corr': False, 'average': 40, 'diff': False, 'sample_rate': 100000000.0, 'acquisition_delay_ns': 500, 'n_columns': 4, 'line_margin': 1, 'bias_T_RC': 100, 'enabled_markers': [], 'differentiate': False, 'dataset_id': 1784, 'dataset_uuid': 1675444655098255110, 'sample_info': "<class 'core_tools.data.SQL.connect.sample_info'>"}