## Slide 1: SQ22-79-5-2-2
Noether Fridge 15-02-2023
from core_tools.data.SQL.connect import set_up_local_storage
project = '2x2d2s_v2'
setup = 'noether_fridge'
sample = 'SQ22-79-5-2-2'
set_up_local_storage('chien', 'chien', 'veldhorst_data', project, setup, sample)

## Slide 2: Charge Noise Data
15-02-2023

## Slide 3: About the sample
2x2d2s
SET Studied for charge noise

## Slide 4: Procedure
1) Measure dc scan of several Coulomb peaks
2) Take 9 peaks and note in a table the voltages of the valleys
3) Choose an ‘optimal currents’ for charge noise measurement on the left flanges an note it in a table
4) For each peak
a. Go in the valley and measure charge noise
b. Increase by steps of 0,05 mV the plunger gate voltage to reach the optimal current
c. Repeat step b. after few seconds to take into account drift
d. Lower the voltage by 4 mV normally in the valley but not sure
f. Repeat a,b,c,d two more times
g. Make a dc scan showing two peaks  The right one is the one that was measured
h. Measure Coulomb diamond
Automatic
Manual

## Slide 5: Technical details
DC measurement Bias : Vdc = 0,5 mV bias x 100 mV/V (Vib module). There does seem to be an offset of about ~1,3mV x 100 mV/V (Vib module)
DC measurement Current Measurement : M1k Module 100 MV/A
A constant current offset has to be removed
It seems that the peak have shifted by a few mV to the left between first large scan and charge noise measurements
So the first valley measurement is not really reliable
There is probably transport through an excited state or cotunelling

## Slide 6: Full Scan
Points Chosen:
optimal_current_a = np.array([400,450,550,650,650,650,650,550,400])*1e-12
valleys_a = [1161,1171,1180,1189,1198,1206,1215,1223,1233]
16764_81067_600255110

## Slide 7: Peak 1 , Current targeted = 400 pA, Voltage valley = 1161 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16764_83346_823255110 | 50 | OK a bit high | 16764_84719_546255110 | 340 | OK small jump
2 | 16764_85332_412255110 | 40 | OK | 16764_86328_173255110 | 400 | OK small jump
3 | 16764_86941_002255110 | 40 | OK | 16764_87636_859255110 | 400 | OK small jump
Start: 15/02/23 at 18h49
End: 15/02/23 at 20h11
Excited states ?
16764_88247_721255110
16764_88268_797255110

## Slide 8
slope = 1.5262128263094385e-06 A/V
0.1754500361342906

## Slide 9: Peak 2 , Current targeted = 450 pA, Voltage valley = 1171 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16764_83346_823255110 | 50 | A bit high | 16764_89435_260255110 | 430 | OK small jump
2 | 16764_90048_161255110 | 40 | OK | 16764_91029_819255110 | 370 | OK a bit high
3 | 16764_92568_974255110 | 40 | OK | 16764_92568_974255110 | 410 | OK
Start: 15/02/23 at 20h18
End: 15/02/23 at 21h32
16764_93179_736255110
16764_93201_636255110

## Slide 10
slope = 1.6583901442856224e-06 A/V
0.16105580010553336

## Slide 11: Peak 3 , Current targeted = 550 pA, Voltage valley = 1180 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16764_93629_225255110 | 65 | Too high | 16764_94364_446255110 | 500-600 | Shaky !
2 | 16764_94977_369255110 | 40 | OK | 16764_96257_195255110 | 450 | Shaky !
3 | 16764_96870_099255110 | 40 | OK | 16764_97697_651255110 | 650 | Shaky and high
Start: 15/02/23 at 21h40
End: 15/02/23 at 22h58
16764_98331_236255110
16764_98308_499255110

## Slide 12
slope = 1.545971087738993e-06 A/V
0.14882224965478538

## Slide 13: Peak 4 , Current targeted = 550 pA, Voltage valley = 1189 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16764_98773_930255110 | 55 | OK a bit high | 16764_99465_540255110 | 650 | A bit high
2 | 16765_00078_459255110 | 45 | OK | 16765_01677_860255110 | 680 | A bit high
3 | 16765_01681_047255110 | 45 | OK | 16765_02414_680255110 | 650 | A bit high
Start: 16/02/23 at 23h06
End: 16/02/23 at 22h58
16765_03025_715255110
16765_03047_674255110
Peak shrinked !

## Slide 14
slope = 1.065148113211051e-06 A/V
0.13556151851127898

## Slide 15: Peak 5 , Current targeted = 650 pA, Voltage valley = 1198 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16765_03474_990255110 | 45 | OK | 16765_04511_225255110 | 670 | High but maybe OK
2 | 16765_05123_995255110 | 45 | OK | 16765_05874_130255110 | 650-280 | Jump maybe 1st part usable
3 | 16765_06486_959255110 | 45 | OK | 16765_07608_542255110 | 650 | High but maybe OK
Start: 16/02/23 at 00h24
End: 16/02/23 at 01h41
16765_03047_674255110
Jump to the next peak !
Peak shrinked !
In practise 1204 mV
Not using it

## Slide 16: Peak 6, Current targeted = 650 pA, Voltage valley = 1206 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16765_08664_436255110 | 45 | OK | 16765_09606_644255110 | 650 | OK maybe a bit high
2 | 16765_10219_561255110 | 50 | OK | 16765_17791_213255110 | 650 | OK
3 | 16765_18404_048255110 | 50 | OK | 16765_19459_293255110 | 750-400 | Jump , 1st part usable
Start: 16/02/23 at 00h24
End: 16/02/23 at 01h41
Jump to the next peak between measurement 1 & 2
its seems
1
2,3
16765_20092_493255110
16765_20070_072255110
Very long = problem ?
2h in between

## Slide 17
slope = 2.425077149759443e-06 A/V
0.1123643186986811

## Slide 18: Peak 7, Current targeted = 650 pA, Voltage valley = 1215 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16765_20525_815255110 | 60 | Too high | 16765_21252_007255110 | 550 | OK
2 | 16765_21864_882255110 | 50 | OK | 16765_22856_021255110 | 650 | OK small drift
3 | 16765_23469_022255110 | 50 | OK | 16765_24246_140255110 | 750 | OK
Start: 16/02/23 at 05h08
End: 16/02/23 at 06h20
16765_24856_997255110
16765_24879_650255110

## Slide 19
slope = 2.424636901069371e-06 A/V
0.12269685627740565

## Slide 20: Peak 8, Current targeted = 550 pA, Voltage valley = 1223 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16765_25314_584255110 | 300 | Not a valley | 16765_26280_094255110 | 350 | Jump to peak bottom at beginning
2 | 16765_26892_886255110 | 50 | OK | 16765_27610_968255110 | 650 | OK
3 | 16765_28223_841255110 | 50 | OK | 16765_29285_895255110 | 600 | OK
Start: 16/02/23 at 06h28
End: 16/02/23 at 07h45
Direction scan
16765_29896_676255110
16765_29918_304255110
NO Charge jump in Coulomb Diamons

## Slide 21
slope = 3.03505867048793e-06 A/V

## Slide 22: Peak 9, Current targeted = 450 pA, Voltage valley = 1233 mV
Iteration | Charge noise Valley uuid | Approx Current (pA) | Comment | Charge noise Slope uuid | Approx Current (pA) | Comment
1 | 16765_30346_876255110 | 50 | OK | 16765_31277_372255110 | 450 | Rather on the peak bottom
2 | 16765_31890_204255110 | 50 | OK | 16765_32616_575255110 | 400 | Rather on the peak bottom
3 | 16765_33229_423255110 | 50 | OK | 16765_33968_321255110 | 450 | Rather on the peak bottom
Start: 16/02/23 at 07h52
End: 16/02/23 at 09h03
Direction scan
16765_34602_060255110
16765_34579_190255110

## Slide 23
slope = 3.070048075238579e-06 A/V
0.11407919054730377