## Slide 1: Si - SiGe - SQ21_160_5,6,7
Marc Botifoll marc.botifoll@icn2.cat
Jordi Arbiol arbiol@icrea.cat

## Slide 2: SQ21_160_6 (6nm): Strain, GPA and plane counting
GPA strain (exx and eyy):
Cell parameter (a_cell) of QW and its standard deviation 5.437±0.002 Å
Cell parameter (a_cell) of the buffer layer and its standard deviation 5.496±0.002 Å
Dilatation of horizontal planes, in y direction: -1.7005±0.0003 %
Dilatation of vertical planes, in x direction: -0.1026±0.0002 %
Measure done in: 315000 pixels
Experimental horizontal planes in the QW: 2.7011±0.0011 Å
Experimental vertical planes in the QW: 1.9410 ±0.0008 Å
Strain horizontal planes (eyy): -0.64±0.05 %
Strain vertical planes (exx): 0.97±0.05 %
Spacing between misfit dislocations every 973±529 planes
Spacing between misfit dislocations of 0.19±0.10 µm
5%
-5%
Si0.69(±0.01) Ge0.31(±0.01)
Si0.97(±0.01) Ge0.03(±0.01)
Si0.69(±0.01) Ge0.31(±0.01)
STEM-HAADF
ϵxx
ϵyy
Plane counting
GPA
Plane counting strain (exx):
Dilatation of vertical planes, in x direction: -0.08±0.04 %
Experimental vertical planes in the QW: 1.9415±0.0012 Å
Strain vertical planes (exx): 1.00±0.07 %
Spacing between misfit dislocations every 1302±1208 planes
Spacing between misfit dislocations of 0.25±0.23 µm
x
y
6.9 nm

## Slide 3: Thickness calculation: SQ21_160_6
-Dilatation of horizontal planes, in y direction: -1.7005±0.0003 %
-Experimental horizontal planes in the QW: 2.7011±0.0011 Å
-4 measurements done, two of 25 (25*2.7011 -> 6.7524nm) planes counted, and two of 26 (26*2.7011 -> 7.02286nm), which average 6.8878nm, with an error of two counted (002) planes = 2*2.7011= 5.4022Å  thickness = 6.9±0.5nm
1 plane (002)
26 planes (002)
1 plane (002)
26 planes (002)